Supplementary material

Figure S1. The gross morphology (top) of polylactide (PLA)-based fibers (PLA), PLA-based fibers containing quercetin (PLA/Q), PLA and polyethylene oxide (PEO)-based fibers (PLA/PEO) and PLA and PEO-based fibers containing quercetin (PLA/PEO/Q) (scale bar 100 µm). The fiber diameter is also presented (bottom; average, max, min and range values in µm).

Figure S2. Physical characterization of polylactide (PLA)-based fibers (PLA). Scanning electron microscopy (SEM) was used to analyze the geometry (A, B) and diameter distribution (C) of PLA-based fibers in acetone and chloroform solution; magnification 5000 (A), magnification 10000 (B). (D) XRD diffractogram of PLA-based fibers. (E) Differential thermal analysis/thermogravimetry (DTA/TG) measurements to analyze heat flow (DTA) and mass change (TG) during heating of PLA-based fibers. (F) The analysis of the contact angle of PLA-based fibers using PGX goniometer.

Figure S3. Physical characterization of PLA-based fibers containing quercetin (PLA/Q). Scanning electron microscopy (SEM) was used to analyze the geometry (A, B) and diameter distribution (C) of PLA/Q in acetone and chloroform solution; magnification 5000 (A), magnification 10000 (B). (D) XRD diffractogram of PLA/Q. (E) Differential thermal analysis/thermogravimetry (DTA/TG) measurements to analyze heat flow (DTA) and mass change (TG) during heating of PLA/Q. (F) The analysis of the contact angle of PLA/Q using PGX goniometer.

Figure S4. Physical characterization of PLA and polyethylene oxide (PEO)-based fibers (PLA/PEO). Scanning electron microscopy (SEM) was used to analyze the geometry (A, B) and diameter distribution (C) of PLA/PEO in acetone and chloroform solution; magnification 5000 (A), magnification 10000 (B). (D) XRD diffractogram of PLA/PEO. (E) Differential thermal analysis/thermogravimetry (DTA/TG) measurements to analyze heat flow (DTA) and mass change (TG) during heating of PLA/PEO. (F) The analysis of the contact angle of PLA/PEO using PGX goniometer.

Figure S5A. AFM-based characterization of PLA-based fibers (PLA). Tapping mode AFM height (top), amplitude (middle) and 3D (bottom) PLA images are shown (scan size 20 µm x 20 µm).

Figure S5B. AFM-based characterization of PLA-based fibers containing quercetin (PLA/Q). Tapping mode AFM height (top), amplitude (middle) and 3D (bottom) PLA/Q images are shown (scan size 20 µm x 20 µm).

Figure S5C. AFM-based characterization of PLA- and PEO-based fibers (PLA/PEO). Tapping mode AFM height and amplitude (top) and 3D (bottom) PLA/PEO images are shown (scan size 20 µm x 20 µm).

Figure S5D. AFM-based characterization of PLA- and PEO-based fibers containing quercetin (PLA/PEO/Q). Tapping mode AFM height (top), amplitude (middle) and 3D (bottom) PLA/PEO/Q images are shown (scan size 20 µm x 20 µm).

Figure S5E. AFM-based analysis of the roughness of PLA, PLA/Q, PLA/PEO and PLA/PEO/Q fibers. Topography of PLA, PLA/Q, PLA/PEO and PLA/PEO/Q surfaces with marked areas for roughness analysis is shown (top). Selected roughness parameters are presented (bottom; Rmax, Rz, Rms, and Ra).

Figure S6. XRD diffractogram of free quercetin (A) and differential thermal analysis/thermogravimetry (DTA/TG) measurements to analyze heat flow (DTA) and mass change (TG) during heating of free quercetin (B).

Figure S7. The Raman spectra of PLA (A), PLA/Q (B), PLA/PEO (C), and PLA/PEO/Q (D). Dry fibers as well as fibers incubated in water for 0, 48, and 96 h were analyzed. (A) The obtained spectra of dry and T0 samples are characteristic for the PLA polymer structure. They are similar to PLA/PEO sample spectra. The characteristic bands can be identified at 2998 cm-1, 2947 cm-1, 2879 cm-1 (C-H stretching vibrations), 1769 cm-1 (C=O stretching), 1456 cm-1, 1387 cm-1 and 1298 cm-1 (CH3 deformation), 1184 cm-1 (C-O-C), 1129 cm-1 (CH3 rocking), 1045 cm-1 (C-CH3), 874 cm-1 (C-COO), 402 cm-1 (C-CO), 310 cm-1 (C-OC and C-CH3), 254 cm-1 (CCO) [1-3]. (B) The obtained spectra are characteristic for the PLA polymer and quercetin structure. The spectral line characteristic for PLA polymer are the same as described for PLA sample. The line characteristic for quercetin present in the spectrum of the fibers: 1656 cm-1, 1614 cm-1, 1558 cm-1, 1321 cm-1, 999 cm-1, 934 cm-1, 847 cm-1, 792 cm-1, 643 cm-1, 598 cm-1, 522 cm-1, 490 cm-1. (C) The obtained spectra are characteristic for the PLA and PEO polymers structure. The characteristic bands can be identified at 2998 cm-1, 2957 cm-1, 2882 cm-1 (C-H stretching vibrations), 1770 cm-1 (C=O stretch), 1445 cm-1, 1388 cm-1 and 1298 cm-1 (CH2 and CH3 deformation), 1184 cm-1 (C-O-C), 1129 cm-1 (CH3 rocking), 1045 cm-1 (C-CH3), 874 cm-1 (C-COO), 408 cm-1 (C-CO), 308 cm-1 (C-OC and C-CH3), 250 cm-1 (CCO) [1-3]. (D) The obtained spectra are characteristic for the PLA, PEO polymers and quercetin structure. The spectral lines characteristic for PLA and PEO polymers are the same as described for PLA/PEO sample. The line characteristic for quercetin present in the spectrum of the fibers: 1659 cm-1, 1615 cm-1 (C=O stretch), 1569 cm-1 (O-H bend), 1319 cm-1 (ring deformation), 997 cm-1 (ring stretch), 934 cm-1 (ring stretch), 846 cm-1 (ring stretch), 788 cm-1 (O-H stretch - ring), 637 cm-1 (ring stretch), 599 cm-1 (ring stretch), 520 cm-1 (ring deform.), 487 cm-1 (ring deform.) [4].

1.	Pandele, Andreea & Constantinescu, Andreea & Radu, Cristian & Miculescu, Florin & Voicu, Ş.I. & Ciocan, Lucian. (2020). Synthesis and Characterization of PLA-Micro-structured Hydroxyapatite Composite Films. Materials. 13. 10.3390/ma13020274.

2.	Bolskis, Evaldas & Adomavičiūtė, Erika & Griskonis, Egidijus. (2022). Formation and Investigation of Mechanical, Thermal, Optical and Wetting Properties of Melt-Spun Multifilament Poly(lactic acid) Yarns with Added Rosins. Polymers. 14. 379. 10.3390/polym14030379.

3.	Blaszczyk-Lezak, Iwona & Maiz, Jon & Sacristan, Javier & Mijangos, Carmen. (2011). Monitoring the Thermal Elimination of Infiltrated Polymer from AAO Templates: An Exhaustive Characterization after Polymer Extraction. Industrial & Engineering Chemistry Research. 50. 10883-10888. 10.1021/ie200826x.

4.	Yasushi Numata, Hiroyuki Tanaka, Quantitative analysis of quercetin using Raman spectroscopy, Food Chemistry, Volume 126, Issue 2, 2011, Pages 751-755, https://doi.org/10.1016/j.foodchem.2010.11.059.

Figure S8. (A) Calibration curve used for the evaluation of quercetin concentrations in aqueous solution upon the incubation of PLA/Q and PLA/PEO/Q in cell-free in vitro systems (Fig. 2A). Several concentrations of quercetin were considered (up to 20 µg/ml) and absorbance was read at 365 nm using an absorbance mode microplate reader. (B) PLA/Q and PLA/PEO/Q-induced apoptosis in osteosarcoma cells (MG-63, U-2 OS and SaOS-2 cells). Cells were treated with the fibers for 48 h. Apoptosis was evaluated using flow cytometry and dual staining approach, namely Annexin V staining and 7-AAD staining. Four subpopulations were distinguished, namely live cells (dual staining-negative), early apoptotic cells (Annexin V-positive), late apoptotic cells (dual staining-positive) and necrotic cells (7-AAD-positive). Representative dot-plots are shown. (C) PLA/Q and PLA/PEO/Q-mediated changes in cell cycle progression in osteosarcoma cells (MG-63, U-2 OS and SaOS-2 cells). Cells were treated with the fibers for 48 h. The phases of cell cycle were studied using DNA content-based analysis of cell cycle using flow cytometry and dedicated DNA staining. Representative histograms are shown. CTR, control conditions; PLA, treatment with polylactide-based fibers; PLA/Q, treatment with polylactide-based fibers containing quercetin; PLA/PEO, treatment with polylactide and polyethylene oxide-based fibers; PLA/PEO/Q, treatment with polylactide and polyethylene oxide-based fibers containing quercetin.

Figure S9. PLA/Q and PLA/PEO/Q-induced oxidative stress (A), Akt and ERK1/2 activation (B) and changes in the levels of HSP70 and HSP90 in osteosarcoma cells (MG-63, U-2 OS and SaOS-2 cells). Cells were treated with the fibers for 48 h (A, B) or 24 h (C). (A) Oxidative stress marker was considered, namely the levels of superoxide. Superoxide levels were assessed using flow cytometry and dihydroethidium staining. Two subpopulations were revealed, namely superoxide-positive (red) and superoxide-negative (blue) cells. Representative histograms are shown. (B) The activation of Akt and ERK1/2 was analyzed as phosphorylation status of Akt and ERK1/2 using flow cytometry and dedicated anti-phospho-Akt and anti-phospho-ERK1/2 antibodies. Cells with single activation (Akt activation or ERK1/2 activation) and dual activation (Akt activation and ERK1/2 activation) were distinguished. Representative dot-plots are shown. (C) Immunofluorescence-based analysis of nuclear and cytoplasmic levels of HSP70 and HSP90 was performed using imaging cytometry and dedicated anti-HSP70 and anti-HSP90 antibodies. Nuclear and cytoplasmic levels of HSP70 and HSP90 are presented as relative fluorescence units (RFU). Box and whisker plots are shown, n = 3, ***p < 0.001, **p < 0.01, *p < 0.05 compared to CTR untreated control (ANOVA and Dunnett’s a posteriori test). CTR, control conditions; PLA, treatment with polylactide-based fibers; PLA/Q, treatment with polylactide-based fibers containing quercetin; PLA/PEO, treatment with polylactide and polyethylene oxide-based fibers; PLA/PEO/Q, treatment with polylactide and polyethylene oxide-based fibers containing quercetin.

Figure S10. (A) PLA/Q and PLA/PEO/Q-induced apoptosis in breast cancer cells (SK-BR-3, MCF-7, MDA-MB-231, MDA-MB-468, Hs 578T, and BT-20 cells). Cells were treated with the fibers for 48 h. Apoptosis was evaluated using flow cytometry and dual staining approach, namely Annexin V and 7-AAD staining. Four subpopulations were distinguished, namely live cells (dual staining-negative), early apoptotic cells (Annexin V-positive), late apoptotic cells (dual staining-positive) and necrotic cells (7-AAD-positive). Representative dot-plots are shown. CTR, control conditions; PLA, treatment with polylactide-based fibers; PLA/Q, treatment with polylactide-based fibers containing quercetin; PLA/PEO, treatment with polylactide and polyethylene oxide-based fibers; PLA/PEO/Q, treatment with polylactide and polyethylene oxide-based fibers containing quercetin. (B) The analysis of fiber hemocompatibility. The biocompatibility of Q-loaded fibers was investigated using in vitro hemolysis test. Whole blood samples were incubated with PLA, PLA/PEO, PLA/Q and PLA/PEO/Q for 24 and 48 h. The absorbance measurements were normalized to CTR (positive control, 100% of hemolysis, treatment with 37.5 mM KCl). Bars indicate SD, n = 3, ***p < 0.001 compared to CTR positive control, KCl-treated blood sample (ANOVA and Dunnett’s a posteriori test). CTR, positive control, KCl-treated blood sample; PLA, treatment with polylactide-based fibers; PLA/Q, treatment with polylactide-based fibers containing quercetin; PLA/PEO, treatment with polylactide and polyethylene oxide-based fibers; PLA/PEO/Q, treatment with polylactide and polyethylene oxide-based fibers containing quercetin.

Table S1. Characteristic bands of free quercetin and quercetin-loaded fibers based on FTIR spectra.

| Free quercetin (cm-1) | Quercetin-loaded fibers (cm-1) |
| --- | --- |
| 1663 | 1656 |
| 1607 | 1600 |
| 1560 | 1564 |
| 1520 | 1517 |

Table S2. Changes in fiber diameter upon incubation in aqueous solution (in distilled water for 0, 48, and 96 h) using Scanning Electron Microscopy (SEM). PLA, polylactide-based fibers; PLA/Q, polylactide-based fibers containing quercetin; PLA/PEO, polylactide and polyethylene oxide-based fibers; PLA/PEO/Q, polylactide and polyethylene oxide-based fibers containing quercetin.

| Material | Time [h] | Diameter [%] |  |
| --- | --- | --- | --- |
|  |  | < 2µm | > 2.01 µm |
| PLA | 0 | 68 | 32 |
|  | 48 | 47 | 53 |
|  | 96 | 87 | 13 |
| PLA/Q | 0 | 72 | 28 |
|  | 48 | 33 | 67 |
|  | 96 | 67 | 33 |
| PLA/PEO | 0 | 0 | 100 |
|  | 48 | 47 | 53 |
|  | 96 | 74 | 27 |
| PLA/PEO/Q | 0 | 82 | 18 |
|  | 48 | 0 | 100 |
|  | 96 | 7 | 93 |